## Slide 1
IITBBS IPR COMMITTEE REVIEW
Novel concrete composition for impact-energy-dissipating crash barriers
Steel-fibre reinforced sintered-fly-ash lightweight aggregate concrete
Haruna Al-Amir Saleh • Pratik Kanungo • Anush K. Chandrappa • Dinakar Pasla
School of Infrastructure | IIT Bhubaneswar | 13 August 2026
Current status: not yet filed • Purpose: IPR approval to proceed with patent filing
Source: inventor-supplied manuscript Fig. 7 — 1:3 barrier impact setup
CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED
01
Notes: OPENING — approximately 45 seconds
• This presentation evaluates an experimentally reduced-to-practice material platform for impact-energy-dissipating crash barriers. It is not a legal patentability opinion.
• The invention team is Haruna Al-Amir Saleh, Pratik Kanungo, Dr Anush K. Chandrappa and Prof Dinakar Pasla, School of Infrastructure, IIT Bhubaneswar.
• The inventors confirm that the patent has not yet been filed. This is the pre-filing presentation to the IIT Bhubaneswar IPR section seeking approval to proceed with professional drafting and filing. A related manuscript was submitted on 18 July 2026, so confidentiality and disclosure timing are critical. Treat this deck accordingly: CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED.
• The central question is not whether the concrete is merely lighter. It is whether the tested combination creates a defensible, multi-mechanism improvement in energy absorption, post-cracking integrity and controlled damage while retaining structural-grade strength.
• The presentation separates measured evidence from proposed occupant-safety benefit. Full-scale vehicle testing is still required before any claim of reduced occupant injury or standards compliance.

## Slide 2
EXECUTIVE THESIS
The value case in one view
CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED
02
A rigid-barrier material that trades brittle force transfer for controlled, multi-scale energy dissipation.
19.4%
lower reported density
LWC15 vs NWC
76%
higher splitting tensile strength
7.60 vs 4.32 MPa
55.3×
prism failure-energy capacity
2,927.8 vs 53.0 N·m
2.0×
scaled-barrier failure energy
2,746 vs 1,373 N·m
01
Protectable technical thesis
Specific material architecture + dual dissipation mechanism + crash-barrier use + tested performance envelope. Claims should centre the integrated system—not isolated known constituents.
02
Commercial value pathway
Precast-compatible manufacturing; lower barrier self-weight; improved damage control; potential transport, deck-load and lifecycle advantages. These benefits require pilot-scale TEA/LCA validation.
03
Evidence boundary
Material and repeated-impact results are strong signals. The 1:3 barrier test used one specimen per mix and did not measure ASI/THIV, vehicle containment or redirection. Occupant benefit remains a testable hypothesis.
Source: Inventor dataset, Al-Amir et al. manuscript (submitted 18 Jul 2026), Tables/Figs 8–12; calculations in accompanying workbook.
Notes: KEY MESSAGE — approximately 60 seconds
• Lead with the evidence: relative to normal-weight concrete, the selected lightweight mixture has 19.4% lower reported density and 75.9% higher splitting tensile strength. In the repeated drop-weight prism test it absorbed 55.3 times the failure energy of NWC.
• At the barrier scale, the one-third model absorbed twice the cumulative pendulum energy before failure and deformed approximately three times as much as the NWC model. That is the most application-relevant result, but it is preliminary because only one barrier per mix was tested.
• The patent thesis should not be “steel fibre is useful” or “lightweight aggregate is useful”; both are known. The potentially protectable value is the integrated composition, the use of SFA and hooked-end fibres in a crash-barrier system, the dual energy-dissipation mechanism, and the demonstrated performance combination.
• Commercially, the material can use conventional concrete/precast infrastructure. The cost per unit of laboratory impact energy is favourable, but no lifecycle cost analysis or environmental life-cycle assessment has yet been performed.
• Do not state that occupant injury has been reduced. Say that the measured deformation and energy absorption support a hypothesis of lower force transmission that must be tested at full scale.

## Slide 3
GLOBAL EVIDENCE
The need is global: safety, materials and circularity intersect
CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED
03
Chart: 
| Upper-middle | Lower-middle | Low | High
Share | 35 | 44 | 13 | 8
92%
of deaths in LMICs
Global road-traffic deaths by country income group, 2021
1.19 M
road deaths/year
WHO 2023; 2021 estimate
50 Gt
sand + gravel/year
UNEP 2022 estimate
4.0 Gt
cement produced, 2024
USGS 2025 • ~0.6 tCO₂/t (IEA)
>1 Gt
coal fly ash/year
IEA CCC 2020; global order
Opportunity: reduce crash severity while substituting a portion of virgin aggregate and clinker-intensive binder inputs. Boundary: this project has not yet completed full-scale crash testing or a product LCA.
Source: WHO, Global Status Report on Road Safety 2023, pp. 4, 14; UNEP, Sand and Sustainability (2022); USGS, MCS—Cement (2025); IEA, Cement (2023); Reid, Carpenter & Masili, IEA CCC/303 (2020).
Notes: GLOBAL CONTEXT — approximately 75 seconds
• The global road-safety burden is about 1.19 million deaths annually. WHO estimates that 92% occur in low- and middle-income countries. The pie chart is a global dataset: 35% upper-middle, 44% lower-middle, 13% low-income and 8% high-income countries.
• At the same time, construction operates at planetary material scale: UNEP estimates 50 billion tonnes of sand and gravel are used each year; USGS estimates about 4.0 billion tonnes of cement were produced in 2024, while IEA reports direct cement-emissions intensity just under 0.6 tonnes of CO₂ per tonne.
• Coal combustion also generates more than one billion tonnes of fly ash annually by order of magnitude. Availability and specification vary regionally, so this figure supports the resource opportunity—not a guaranteed feedstock claim.
• The invention sits at the intersection of three needs: safer roadside infrastructure, lower self-weight and virgin-aggregate demand, and productive use of industrial by-products.
• Be explicit about the environmental boundary. The mix uses GGBS and sintered fly ash aggregate, but sintering consumes energy and the high steel-fibre dosage has embodied impacts. A comparative, region-specific LCA is required before claiming a net carbon reduction.
• Transition: global need alone does not establish novelty. The next slide maps the prior-art trade space.

## Slide 4
LANDSCAPE
Prior art leaves an unresolved multi-objective gap
CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED
04
Approach | Containment / strength | Energy dissipation | Damage control | Scale / cost | Residual gap
Rigid NWC barrier | High | Low–moderate | Brittle / debris risk | Mature | Harsh impact pulse
Steel / cable | System-dependent | High via deflection | Repair after impact | Corrosion / clear zone | Space + maintenance
Rubberised + fibre | Strength trade-off | Improved | Improved | Processing complexity | Durability / scale
UHPC / ECC | Very high | Mix-dependent | Good crack control | High material cost | Stiffness / economics
Lightweight barrier concepts | Demonstrated in prior art | Potential | Design-specific | Limited adoption | No SFA–fibre proof set
This invention | M40+ in tested mixes | High in repeated impact | Controlled cracking observed | Precast-compatible | Full-scale proof pending
PATENT POSITIONING
Avoid a broad “first lightweight concrete barrier” assertion: lightweight-concrete barrier concepts appear in conference literature. Centre novelty on the specific integrated composition, SFA function, hooked-fibre crack control, quantified synergy and manufacturing/control envelope.
Source: Zain & Mohammed (2015); Raj et al. (2020), ASCE J. Mater. Civ. Eng.; Shen et al. (2014), Constr. Build. Mater.; Bonin et al. (2004), II Int’l Congress SIIV proceedings; Grzebieta et al. (2005), 19th ESV Conference proceedings; Xue et al. (2025).
Notes: PRIOR ART AND DIFFERENTIATION — approximately 90 seconds
• Conventional rigid concrete barriers are mature and effective for containment, but their low deflection can create a severe vehicle pulse, and brittle damage can generate debris under severe impact.
• Flexible and semi-rigid systems dissipate energy through global deflection, but require working width and post-impact repair. Rubberised, UHPC and ECC concepts each solve part of the problem, while introducing strength, cost, stiffness or processing trade-offs.
• A critical patentability point: prior conference literature includes lightweight concrete road-safety barrier concepts—for example Bonin and co-authors at the 2004 SIIV congress. Therefore, do not rely on a sweeping “first lightweight barrier” proposition.
• The narrower and more defensible thesis is the integrated OPC/GGBS/SFA/hooked-end-fibre composition, its use as the load-bearing crash-barrier material, and the observed synergy: structural strength, lower reported density, major post-cracking impact resistance and controlled fragmentation.
• The literature and patent searches documented by the inventors are preliminary. A professional claim-by-claim patentability and freedom-to-operate search is still required, including composition ranges, SFA manufacture/specification, fibre geometry and barrier-system claims.

## Slide 5
TECHNICAL CONCEPT
Invention architecture: three functions, one controlled response
CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED
05
A
SFA lightweight aggregate
Porous particle crushing + internal damping
B
Hooked-end steel fibre
Crack bridging + debonding + pull-out
C
OPC + 20% GGBS matrix
M40+ strength + fibre/aggregate load transfer
DESIGNED IMPACT RESPONSE
01
Crack initiation
Fibres redistribute tensile stress and delay localisation.
02
Controlled deformation
Aggregate crushing and fibre pull-out consume energy.
03
Residual integrity
Bridging restrains large fragments and preserves load path.
04
Lower transmitted peak force
Mechanistic hypothesis; requires vehicle-level validation.
Proposed inventive step: an intentionally semi-energy-absorbing rigid barrier in which the material—not only the barrier geometry—dissipates collision energy while retaining structural-grade strength.
Source: Inventor disclosure (16 Jul 2026), §§Description/Novelty/Inventiveness; Wang & Wang (2013); Nadesan & Dinakar (2017); Sahoo et al. (2020). Mechanism diagram is an author synthesis.
Notes: MECHANISM — approximately 80 seconds
• The concept intentionally combines three functions. First, the porous SFA can crush locally and contribute internal damping. Second, hooked-end steel fibres bridge cracks and dissipate energy through progressive debonding, friction and pull-out. Third, the cement–GGBS matrix provides the structural-grade load path and transfers stress into the aggregate and fibres.
• The expected sequence is crack initiation, distributed bridging and controlled deformation, followed by progressive internal energy dissipation and improved residual integrity.
• This mechanism is consistent with published composite-material literature, but the invention’s value proposition is the protected integration and crash-barrier application supported by the experimental results.
• Phrase the final outcome carefully. The experiments demonstrate increased specimen deformation and cumulative absorbed energy. They do not directly demonstrate a lower peak vehicle force, reduced ASI or reduced occupant injury. Those remain mechanistically plausible validation targets.
• For claim drafting, consider separate families covering composition ranges, mixing/conditioning controls, a barrier article made from the composition, and functionally linked performance features where legally supportable.

## Slide 6
EXPERIMENTAL PROGRAMME
Evidence ladder: from constituents to a scaled barrier
CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED
06
01
Constituent characterisation
XRF, physical properties, SFA absorption, fibre geometry
02
Mixture screening
NWC + 4 LWC variants; 0–1.5% fibre by volume
03
Static performance
Reported density, slump, 28 d compression and split tension
04
Repeated impact
13.5 kg drop hammer; N₁/N₂, energy, acceleration → displacement
05
Barrier-scale validation
1:3 New Jersey models; 40 kg pendulum; NWC vs LWC15
REPLICATION / UNCERTAINTY
The methods report 3 cubes + 3 cylinders per mix and 4 beams cast per mix; impact tables do not report dispersion for N₁/N₂. Barrier validation used one specimen per material. Treat barrier-scale effect sizes as preliminary, not population estimates.
Source: Al-Amir et al. manuscript, Experimental Program and Testing Methods; inventor disclosure, Experimental Data Analysis. Sample-count interpretation is based on the stated casting plan.
Notes: EXPERIMENTAL LOGIC — approximately 75 seconds
• The evidence was built in five layers: constituent characterization, mixture screening, static mechanical tests, repeated drop-weight impact testing and a one-third-scale barrier comparison.
• Four lightweight mixtures were evaluated with fibre volume increasing from zero to 1.5%, alongside an M40 normal-weight reference.
• Static tests provide the strength and density boundary. The repeated impact test provides the key post-cracking energy evidence. Acceleration signals were processed to derive displacement. The selected highest-performing mixture was then used in a New Jersey barrier model and compared with NWC.
• This is a coherent reduction-to-practice chain and is valuable for enablement. However, the uncertainty reporting is incomplete. The article states that three cubes, three cylinders and four beams were cast per mix, but the impact result tables do not provide N1/N2 dispersion. Only one NWC and one selected lightweight barrier were cast.
• The deck therefore uses measured ratios as experimental observations—not as statistically generalized performance guarantees.

## Slide 7
TESTED EMBODIMENTS
Tested material design: a fibre-content performance ladder
CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED
07
Mix | OPC | GGBS | Water | Fine agg. | Nat. coarse | SFA | Steel fibre | PCE
NWC | 338.8 | 87.4 | 173.6 | 795.6 | 948.8 | — | — | 1.9
LWC00 | 422.4 | 105.6 | 195.2 | 466.5 | — | 596.3 | — | 2.8
LWC05 | 422.4 | 105.6 | 195.2 | 466.5 | — | 596.3 | 39.2 | 2.8
LWC10 | 422.4 | 105.6 | 195.2 | 466.5 | — | 596.3 | 78.5 | 2.8
LWC15 | 422.4 | 105.6 | 195.2 | 466.5 | — | 596.3 | 117.8 | 2.8
All constituent quantities in kg/m³. Extra-water quantity intentionally omitted pending method correction.
SELECTED EMBODIMENT • LWC15
• 1.5% fibre by concrete volume • 20% GGBS replacement of total binder • 100% SFA substitution for natural coarse aggregate • Hooked fibre: 30 mm × 0.5 mm; aspect ratio 60 • Reported density: 1,987 kg/m³ • 28 d compressive strength: 55.4 MPa
SCALed barrier mix
Source: Al-Amir et al. manuscript, Tables 4–6 and chart caches. Density terminology retained as “reported density”; the source alternates between wet and dry density. Exact extra-water protocol omitted by user instruction.
Notes: TESTED EMBODIMENTS — approximately 70 seconds
• The experimental programme isolates the effect of the lightweight aggregate and the progressive addition of crack-bridging reinforcement.
• NWC is the structural reference. LWC00 establishes what the porous lightweight aggregate does without fibre. LWC05, LWC10 and LWC15 then trace the fibre-content response.
• LWC15 was selected for the barrier comparison because it maximized repeated-impact endurance and cost per unit of absorbed impact energy while maintaining strength above the M40 requirement.
• The source document contains an unresolved method inconsistency: one passage states that compensation water was added, another says it was not added directly, and the final table lists an extra-water quantity. At the user’s direction, this deck omits that quantity rather than silently choosing one version.
• The source also alternates between “wet” and “dry” density. Accordingly, the deck uses the neutral term “reported density.” Confirm the measurement basis before patent examples, specifications or publications are finalized.

## Slide 8
MEASURED PERFORMANCE
Static performance clears the structural gate
CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED
08
Chart: kg/m³
| NWC | LWC00 | LWC05 | LWC10 | LWC15
Reported density | 2466 | 1885 | 1923 | 1951 | 1987
Reported density
Chart: MPa
| NWC | LWC00 | LWC05 | LWC10 | LWC15
Compression | 49.62 | 51.1 | 53.7 | 56.8 | 55.4
28 d compressive strength
Chart: MPa
| NWC | LWC00 | LWC05 | LWC10 | LWC15
Split tension | 4.32 | 3.36 | 4.77 | 5.92 | 7.6
28 d splitting tensile strength
LWC15 density −19.4%
LWC10 max = 56.8 MPa
LWC15 tension +76%
Workability trade-off: slump fell from 165 mm (LWC00) to 87 mm (LWC15); fibre dispersion and compaction are scale-up control points.
Source: Inventor dataset, manuscript Fig. 8 and Fig. 9 native chart caches. Values shown as supplied; no independent raw-data audit. Three cube/cylinder specimens per mix were stated in the casting plan.
Notes: STATIC RESULTS — approximately 75 seconds
• The material clears the first gate: all mixtures are reported above the M40 target used for rigid crash barriers in the source.
• The selected LWC15 mixture has a reported density of 1,987 kg per cubic metre versus 2,466 for NWC—a 19.4% reduction. Because the manuscript alternates between wet and dry density, describe this as the reported value until the test basis is confirmed.
• Compressive strength is not the main source of the impact benefit, but it is preserved. LWC10 has the maximum measured value at 56.8 MPa; LWC15 remains at 55.4 MPa, 11.7% above NWC.
• The more important shift is tensile: LWC15 reaches 7.60 MPa versus 4.32 MPa for NWC, a 75.9% increase. This supports crack bridging and post-cracking integrity.
• The manufacturing trade-off is workability. Slump decreases to 87 mm at the highest fibre content. Mixing energy, fibre addition rate, moisture condition and compaction therefore belong in the process know-how and quality-control package.

## Slide 9
IMPACT METHODOLOGY
Repeated-impact method captures post-cracking endurance
CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED
09
100 × 100 × 500 mm beam • 400 mm support span
13.5 kg
drop mass
100 mm
drop height
13.24 J
energy / blow
N₁ / N₂
first crack / failure
SIGNAL PIPELINE
detrend
4th-order zero-phase HP filter, 3 Hz
integrate → v
drift correct
integrate → x
Energy metric = mgh × number of blows; repeated impact emphasizes residual toughness.
Source: Experimental photo: inventor-supplied manuscript Fig. 4. Method: ACI 544.2R-89 adapted to prismatic beams; manuscript Testing Methods, Eqs. 1–2 and signal-processing description.
Notes: REPEATED-IMPACT METHOD — approximately 75 seconds
• The prism test uses a 13.5-kilogram hammer dropped 100 millimetres onto a simply supported 100-by-100-by-500-millimetre beam. Each impact supplies approximately 13.24 joules.
• N1 is the number of blows to the first visible crack; N2 is the number to complete failure. Multiplying the counts by mgh gives first-crack and failure energy.
• This test is especially useful for the invention because the differentiating mechanism is expected after cracking. The gap N2 minus N1 is a direct, if simplified, indicator of residual post-cracking endurance.
• An accelerometer recorded the first-impact response. The manuscript describes linear detrending, a fourth-order zero-phase Butterworth high-pass filter at 3 hertz, trapezoidal integration, drift correction and a second integration to derive displacement.
• This is technically stronger than relying only on compressive strength. However, repeated low-velocity drop-weight tests are screening tests—not a substitute for a full-scale oblique vehicle–barrier crash under MASH, EN 1317 or the applicable IRC protocol.

## Slide 10
PRISM IMPACT RESULTS
Steel fibres transform post-cracking impact endurance
CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED
10
Chart: 
| NWC | LWC00 | LWC05 | LWC10 | LWC15
Value | 52.97 | 26.49 | 264.87 | 595.96 | 2927.81
Failure energy, E₂ (N·m)
Chart: blows
| NWC | LWC00 | LWC05 | LWC10 | LWC15
First crack N₁ | 2 | 1 | 5 | 15 | 35
Failure N₂ | 4 | 2 | 20 | 45 | 221
Impact counts
55.3× vs NWC
110.5× vs plain LWC
N₂ = 221 blows
186 post-crack blows
Source: Inventor dataset, manuscript Table 8. E₂ = mgh × N₂. Ratios calculated from supplied values; impact-count variability/replicate distribution is not reported in the table.
Notes: PRISM IMPACT RESULTS — approximately 80 seconds
• Plain lightweight concrete is more brittle than NWC in this test: LWC00 fails after two blows and absorbs 26.49 newton-metres.
• Progressive crack-bridging reinforcement changes the response nonlinearly. The three reinforced variants reach 264.9, 596.0 and 2,927.8 newton-metres at failure, respectively.
• Relative to NWC, LWC15 absorbs 55.3 times the cumulative failure energy. Relative to the plain lightweight control, the factor is 110.5. These very large ratios are driven by post-cracking endurance rather than a comparable increase in compressive strength.
• LWC15 cracks after 35 blows but does not fail until 221 blows, leaving 186 blows in the post-cracking phase. This directly supports the crack-bridging and fibre pull-out mechanism.
• Use the magnitude as strong experimental evidence, but avoid implying a universal material factor. The table does not report dispersion for N1 and N2, and drop-weight impact counts often show high variability. Repeat testing with raw specimen-level data and a suitable statistical model should be a next-step validation task.

## Slide 11
DYNAMIC RESPONSE
Deformation reveals the transition from brittle to ductile response
CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED
11
Chart: mm
| NWC | LWC00 | LWC05 | LWC10 | LWC15
Peak displacement | 0.28 | 0.08 | 0.14 | 0.85 | 0.71
Peak displacement after first impact
Porous SFA
Hooked fibres
Controlled crack path
CRUSH
porous aggregate consumes local energy
BRIDGE
fibres transfer stress across opening cracks
PULL OUT
friction extends the failure process
HOLD
reinforcement restrains large fragments
LWC10 has the highest first-impact displacement (0.85 mm); LWC15 is slightly stiffer (0.71 mm) yet vastly more durable under repeated impact.
Source: Inventor dataset, manuscript Table 9 and material/failure photos (Figs. 2 and 10). Mechanism supported by Wang & Wang (2013), Gao et al. (1997) and Sahoo et al. (2020). Error values supplied: SD 0.005–0.0686 mm.
Notes: DEFORMATION AND MECHANISM — approximately 75 seconds
• Peak displacement after the first impact rises sharply with reinforcement. The intermediate high-reinforcement variant reaches 0.85 millimetres and the selected variant reaches 0.71, compared with 0.28 for NWC and only 0.08 for plain LWC.
• The lower displacement of plain LWC should not be interpreted as superior stiffness. In the context of its immediate failure, it indicates a brittle, low-deformation response.
• The selected variant is slightly less deformable than the preceding variant on the first impact, plausibly because the denser reinforcement network increases stiffness. Yet it has vastly greater repeated-impact endurance. First-impact displacement and cumulative post-cracking toughness are different response dimensions.
• The material mechanism is a coupled sequence: SFA crushing, fibre bridging, debonding and frictional pull-out, followed by restraint of large fragments.
• The source supplies standard deviations for displacement; a future analysis should present full time histories, filtering sensitivity, uncertainty bands and independent displacement verification, because double integration of acceleration is sensitive to drift and cutoff selection.

## Slide 12
TECHNO-ECONOMICS
The optimum is expensive per m³—but efficient per absorbed joule
CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED
12
Chart: ₹/m³
| NWC | LWC00 | LWC05 | LWC10 | LWC15
Material cost | 4945.24 | 4411.62 | 8336.62 | 12261.62 | 16191.62
Material cost
Chart: ₹/(N·m)
| NWC | LWC00 | LWC05 | LWC10 | LWC15
Cost / failure energy | 93.36 | 166.54 | 31.47 | 20.57 | 5.53
Laboratory cost / impact energy
LWC15 cost = 3.27× NWC
Steel fibre dominates cost
Unit impact value = 16.9× better
₹5.53 per N·m
Source: Inventor dataset, manuscript Tables 7 and 10. Local material prices × mix quantities; cost/energy uses prism E₂. Excludes labour, transport, curing, reinforcement, fabrication, repair, service life, inflation and test uncertainty.
Notes: TECHNO-ECONOMIC RESULT — approximately 80 seconds
• The selected lightweight variant is not the cheapest concrete. Its inventor-estimated material cost is about 16,192 rupees per cubic metre, 3.27 times NWC, primarily because of the high steel-fibre dosage.
• The relevant engineering denominator is failure energy. When the reported prism impact capacity is included, LWC15 costs 5.53 rupees per newton-metre versus 93.36 for NWC—about 16.9 times better on this laboratory metric.
• This supports selection of LWC15 for the barrier test and creates a compelling value narrative: pay more per unit volume, receive substantially more post-cracking impact capacity.
• Keep the boundary explicit. This is not a full barrier cost, lifecycle cost or cost-benefit analysis. It omits reinforcement, formwork, labour, transport, curing, installation, repair frequency, downtime and uncertainty. Prices are local and time-specific.
• The commercial study should therefore compare complete installed systems and include lower transport mass, bridge-deck dead load, expected repair after impact, quality-control cost, industrial-aggregate logistics and any savings from modular precast deployment.

## Slide 13
SCALED VALIDATION
Application-scale test: 1:3 New Jersey barrier under pendulum impact
CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED
13
Full-scale and 1:3 cross-section / reinforcement geometry
Pendulum rig: restrained specimen; rear-face accelerometer
40 kg
impactor
0.35 m
vertical rise
≈137.3 J
energy / blow
1 each
barrier / mix
Source: Inventor-supplied manuscript Figs. 5–7; Testing Methods. Geometry scaled 1:3 using dimensional similarity; energy per blow = 40 × 9.81 × 0.35 ≈ 137.3 J. One NWC and one LWC15 barrier were tested.
Notes: SCALED BARRIER TEST — approximately 80 seconds
• To move beyond material coupons, the team fabricated one-third-scale New Jersey-profile barriers using NWC and the selected LWC15 mixture.
• The dimensions were reduced by a factor of three, and a pendulum rig applied repeated impact at mid-height. The impactor mass was 40 kilograms, the vertical rise 0.35 metres and the energy approximately 137.3 joules per blow.
• An accelerometer on the rear face captured the response for the same filtering and integration workflow used in the beam tests.
• This experiment is valuable as an application-scale proof of concept and supports reduction to practice. It also provides comparative failure patterns and cumulative impact energy.
• It is not a standards-compliant crash test. Geometric similarity alone does not guarantee similitude of strain rate, fracture, reinforcement bond, contact, mass, velocity and gravity effects. The specimen was restrained, and there was no vehicle to evaluate containment, redirection, wheel climb, rollover, occupant compartment intrusion, ASI or THIV.
• Also note the sample size: one barrier per material. Treat the result as preliminary but decision-relevant.

## Slide 14
BARRIER RESULTS
Scaled-barrier validation preserves the direction of benefit
CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED
14
Chart: N·m
| NWC | LWC15
Failure energy | 1373 | 2746
Energy to failure
Chart: mm
| NWC | LWC15
Deformation | 4.22 | 12.7
Peak deformation
2.0×
failure energy
3.01×
deformation
20 vs 10
blows to failure
Fragmentation observation is qualitative: LWC15 showed finer, more distributed debris; particle-size/mass and ejection-velocity measurements are still required.
Source: Inventor dataset, manuscript Tables 11–12 and Fig. 16. NWC: N₂=10, E₂=1,373 N·m, 4.22 mm; LWC15: N₂=20, E₂=2,746 N·m, 12.70 mm. n=1 barrier per mix.
Notes: BARRIER RESULTS — approximately 90 seconds
• The application-scale result points in the same direction as the prism tests. The NWC barrier failed after 10 blows and 1,373 newton-metres; LWC15 reached 20 blows and 2,746 newton-metres—exactly twice the cumulative impact energy in the reported setup.
• Peak deformation increased from 4.22 to 12.70 millimetres, a factor of approximately 3.01. Controlled deformation is consistent with the intended energy-dissipation philosophy.
• The failure photographs show a broader, more brittle crack and large localized fragments in NWC, while LWC15 exhibits a narrower crack path and finer, more distributed debris after more impacts.
• That fragmentation finding is qualitative. A stronger patent and commercialization evidence package should sieve and weigh debris, map crack width and density, measure ejection velocity, and assess residual load capacity after prescribed impacts.
• Because n equals one per mix, do not attach confidence intervals or claim a guaranteed two-times product performance. State that the single comparative barrier experiment reproduced the direction of the material-level benefit and justifies replicated/full-scale validation.

## Slide 15
IP EVIDENCE MAP
Measured evidence maps to a layered patent strategy
CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED
15
Evidence | Observed LWC15 result | Supports | Confidence
Reported density | 1,987 kg/m³; −19.4% vs NWC | Lightweight article / transport value | Medium*
Compressive strength | 55.4 MPa; M40+ | Structural-use enablement | High
Split tensile | 7.60 MPa; +76% | Fibre-bridging function | High
Prism failure energy | 2,927.8 N·m; 55.3× NWC | Unexpected technical effect | Medium
Scaled barrier | 2,746 N·m; 2.0× NWC | Barrier-use embodiment | Preliminary
Fragmentation | Finer / distributed debris observed | Controlled-damage function | Preliminary
ILLUSTRATIVE CLAIM STACK
A
Composition
OPC / GGBS / SFA / hooked-fibre ranges
B
Process
conditioning, sequence, dispersion and QC
C
Barrier article
profile + reinforcement + invented concrete
D
Performance
density / strength / impact / damage envelope
E
System use
precast transport-safety applications
* Density basis must be corrected.
Source: Evidence: inventor dataset. Claim structure is a technical drafting aid only—not legal advice. Patentability/FTO requires professional searching, claim construction and jurisdiction-specific counsel.
Notes: EVIDENCE-TO-CLAIM MAP — approximately 90 seconds
• This slide separates what is measured from what it may support in a patent application.
• Strength and splitting tensile data provide the strongest conventional evidence. The repeated-impact result may support an unexpected technical effect, but its uncertainty and test adaptation should be disclosed accurately.
• The barrier-scale result supports an article-of-manufacture embodiment and utility, while remaining preliminary due to n equals one and the absence of a standards-compliant vehicle test.
• A layered filing strategy can include: composition ranges; a process claim around moisture conditioning, mixing sequence, fibre dispersion and quality control; a barrier article made from the material; and carefully drafted functional/performance limitations where enabled.
• Avoid relying only on a narrow point recipe; include supported ranges and fallback positions around binder fraction, SFA substitution, fibre geometry/dosage and performance windows. Do not invent ranges not supported by the notebooks and experiments.
• Before filing, reconcile the water protocol and density terminology, preserve raw data and notebooks, and complete a professional patentability/FTO search. This slide is a technical aid and not legal advice.

## Slide 16
TRANSLATION ROADMAP
De-risking plan: convert a laboratory signal into a certifiable product
CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED
16
NOW
1
Protect
File before disclosure; professional search; lock data provenance
0–6 m
2
Reproduce
Resolve method conflicts; replicate barrier tests; quantify debris
6–12 m
3
Model + age
Calibrate FE; fatigue/repeat impact; chloride, fire and weather
12–24 m
4
Full-scale certify
Vehicle crash: containment, redirection, ASI/THIV and debris
24–36 m
5
Pilot + license
Precast QA, field demonstration, LCA/TEA and partner transfer
TOP RISKS
!
Full-scale vehicle response
!
Fibre workability / balling
!
SFA moisture + variability
!
Durability / corrosion
!
Installed-system cost
!
Patent landscape / disclosure timing
Source: Roadmap synthesizes inventor questionnaire/technology profile and validation gaps against IRC:119-2015, EN 1317/MASH-style evaluation principles, and peer-reviewed barrier crash-test literature. Indicative timing only.
Notes: TRANSLATION ROADMAP — approximately 90 seconds
• The immediate action is protection: reconcile the technical record, complete professional searching and file before any publication, conference presentation, industry pitch or external distribution.
• In the first six months, repeat the key tests with specimen-level data, quantify uncertainty, resolve the method and density conflicts, replicate barrier specimens and turn fragmentation into a measured particle-size, mass and velocity dataset.
• In parallel, calibrate an LS-DYNA or ABAQUS vehicle–barrier model against the experiments, and add durability, corrosion, environmental exposure, repeated-impact and repairability studies.
• The decisive commercialization gate is a full-scale vehicle crash conducted to the required jurisdictional standard. It must evaluate containment, redirection, stability, debris, occupant compartment performance and occupant-risk measures such as ASI or THIV where applicable.
• A pilot then needs precast quality controls, fibre-dispersion inspection, SFA moisture/specification limits, a full installed-system cost model and comparative LCA.
• Candidate partners listed by the inventors include CRRI, MoRTH/NHAI, state PWDs, precast manufacturers, barrier suppliers and major infrastructure contractors.

## Slide 17
RECOMMENDATION
Decision request: approve patent filing and staged validation
CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED
17
The evidence justifies IPR approval to proceed with a focused patent filing— not yet a certified occupant-safety claim.
55.3×
prism E₂ vs NWC
2.0×
scaled barrier E₂
16.9×
lab unit-impact value
IPR DECISIONS REQUESTED
1
Approve patent filing
Authorize search, drafting and filing
2
Maintain confidentiality
Coordinate manuscript release after filing
3
Endorse validation plan
Replicates, debris metrics, FE and full-scale crash
4
Enable technology transfer
Controlled CRRI / NHAI / precast engagement
BOTTOM LINE
Approve filing now; retain full-scale occupant-risk validation as the commercial release gate.
Source: Recommendation based on inventor-supplied evidence and inventor-confirmed pre-filing status as of 13 Aug 2026. No legal, safety-certification or investment assurance is implied.
Notes: CLOSE — approximately 60 seconds
• The recommendation to the IIT Bhubaneswar IPR section is to approve proceeding with a focused patent filing. The team has reduced the concept to practice and demonstrated a distinctive combination of lower reported density, retained structural strength, major repeated-impact endurance and a positive one-third-scale barrier result.
• The evidence does not yet support a certified occupant-safety claim. The commercial release gate must be a full-scale standards-compliant vehicle test with occupant-risk, containment, redirection, stability and debris criteria.
• Four IPR decisions are requested: approve professional prior-art searching, drafting and filing; maintain confidentiality and coordinate manuscript release; endorse a staged validation programme; and enable controlled engagement with crash-test and precast partners.
• The claim strategy should protect the integrated platform rather than a single recipe: material composition and ranges, process controls, a barrier article, and the use/performance relationship where legally enabled.
• Final line: approve protection now, validate the occupant benefit next, and commercialize only after the full-scale safety gate is passed.

## Slide 18
SOURCES
References & primary sources (1/2)
CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED
18
1 Al-Amir, H.; Kanungo, P.; Chandrappa, A.K.; Pasla, D. (2026). Novel Steel-Fiber Reinforced Sintered Fly Ash Light Weight Aggregate Concrete for Crash Barrier Applications. Inventor-supplied manuscript; submitted 18 Jul 2026.
2 IIT Bhubaneswar invention team (2026). Invention and Technology Disclosure Form: Novel Concrete Composition for Impact Energy Dissipating Crash Barriers, dated 16 Jul 2026; Questionnaire; Technology Profile.
3 World Health Organization (2023). Global Status Report on Road Safety 2023. https://www.who.int/publications/i/item/9789240086517
4 UNEP (2022). Sand and Sustainability: 10 Strategic Recommendations to Avert a Crisis. https://wedocs.unep.org/20.500.11822/38362
5 U.S. Geological Survey (2025). Mineral Commodity Summaries 2025—Cement. https://pubs.usgs.gov/periodicals/mcs2025/mcs2025-cement.pdf
6 International Energy Agency (2023). Cement—Tracking Clean Energy Progress. https://www.iea.org/energy-system/industry/cement
7 Reid, I.; Carpenter, A.M.; Masili, A. (2020). Beneficial Uses of Coal Fly Ash. IEA Clean Coal Centre, CCC/303, ISBN 978-92-9029-626-3.
8 IRC:119-2015. Guidelines for Traffic Safety Barriers. Indian Roads Congress, New Delhi.
9 IRC:6-2016. Standard Specifications and Code of Practice for Road Bridges. Indian Roads Congress.
10 ACI 211.2-98. Standard Practice for Selecting Proportions for Structural Lightweight Concrete. American Concrete Institute.
11 ACI 544.2R-89. Measurement of Properties of Fiber Reinforced Concrete. American Concrete Institute.
12 IS 9142 (Part 2):2018. Artificial Lightweight Aggregates—Sintered Fly Ash Aggregate. Bureau of Indian Standards.
13 IIT Bhubaneswar visual identity/logo: https://www.iitbbs.ac.in/ (accessed Aug 2026).
Notes: REFERENCE SLIDE — do not normally read aloud.
• These are the primary inventor documents, global datasets and design/test standards used in the presentation.
• The inventor manuscript is not represented as published or peer reviewed. It is identified as an inventor-supplied manuscript submitted on 18 July 2026.
• The WHO global road-death distribution, UNEP materials estimate, USGS cement-production estimate and IEA cement-emissions context are independently sourced.
• Confirm the current editions and legal applicability of IRC, BIS, ACI, MASH and EN 1317 requirements with the intended certification authority before test planning or product claims.

## Slide 19
SOURCES
Peer-reviewed literature & proceedings (2/2)
CONFIDENTIAL • PRE-FILING IITBBS IPR COMMITTEE EVALUATION • NOT YET FILED
19
14 Raj, A.; Nagarajan, P.; Pallikkara, S.A. (2020). Application of Fiber-Reinforced Rubcrete for Crash Barriers. J. Mater. Civ. Eng. 32(12), 04020358. doi:10.1061/(ASCE)MT.1943-5533.0003454.
15 Shen, W. et al. (2014). Investigation on the safety concrete for highway crash barrier. Constr. Build. Mater. 70, 394–398. doi:10.1016/j.conbuildmat.2014.07.060.
16 Zain, M.F.M.; Mohammed, H.J. (2015). Concrete road barriers subjected to impact loads: an overview. Lat. Am. J. Solids Struct. 12, 1824–1858. doi:10.1590/1679-78251783.
17 Wang, H.T.; Wang, L.C. (2013). Static and dynamic properties of steel fiber reinforced lightweight aggregate concrete. Constr. Build. Mater. 38, 1146–1151. doi:10.1016/j.conbuildmat.2012.09.016.
18 Sahoo, S.; Selvaraju, A.K.; Suriya Prakash, S. (2020). Mechanical characterization of structural lightweight aggregate concrete made with SFA and synthetic fibres. Cem. Concr. Compos. 113, 103712. doi:10.1016/j.cemconcomp.2020.103712.
19 Nadesan, M.S.; Dinakar, P. (2017). Mix design and properties of fly ash waste lightweight aggregates in structural lightweight concrete. Case Stud. Constr. Mater. 7, 336–347. doi:10.1016/j.cscm.2017.09.005.
20 Kim, W. et al. (2019). Evaluation of concrete barriers with novel shock absorbers subjected to impact loading. Arch. Civ. Mech. Eng. 19, 657–671. doi:10.1016/j.acme.2019.01.004.
21 Yang, J. et al. (2019). Crash performance evaluation of a new movable median guardrail. Eng. Struct. 182, 459–472. doi:10.1016/j.engstruct.2018.12.090.
22 Abid, S.R. et al. (2020). Repeated drop-weight impact tests on self-compacting concrete reinforced with microsteel fiber. Heliyon 6, e03198. doi:10.1016/j.heliyon.2020.e03198.
23 Li, N.; Park, B.B.; Lambert, J.H. (2018). Effect of guardrail on reducing fatal and severe injuries on freeways. J. Transp. Saf. Secur. 10(5), 455–470. doi:10.1080/19439962.2017.1297970.
24 Grzebieta, R.H. et al. (2005). Roadside Hazard and Barrier Crashworthiness Issues. Proc. 19th Int’l Technical Conf. on Enhanced Safety of Vehicles, Paper 05-0149-O, NHTSA.
25 Bonin, G.; Cantisani, G.; Loprencipe, G.; Ranzo, A. (2004). Road safety barriers with short elements of lightweight concrete. Proc. II Int’l Congress SIIV—New Technologies and Modelling Tools for Roads.
26 Iqbal, M. (2011). Vehicular Impact Loading and Barrier Design. ACI Symposium Publication SP-281, 1–16. doi:10.14359/51683612.
27 Pachocki, Ł.; Bruski, D. (2020). Modeling, simulation and validation of a TB41 concrete restraint-system crash test. Arch. Civ. Mech. Eng. doi:10.1007/s43452-020-00065-7.
Notes: REFERENCE SLIDE — do not normally read aloud.
• This list deliberately includes both reputable journal literature and conference/symposium proceedings relevant to concrete-barrier crashworthiness and lightweight material concepts.
• Bonin et al. is particularly important for novelty framing because it shows that lightweight-concrete road-safety barrier concepts existed before this invention. The proposed patent position must therefore be narrower and evidence-led.
• The literature supports the plausibility of fibre bridging, lightweight-aggregate energy dissipation and the importance of occupant-risk metrics; it does not independently validate the exact invented formulation.
• A patent professional should expand this literature review into a jurisdiction-specific patentability and freedom-to-operate search before claims are finalized.